| Physical and Chemical Properties |  |
| --- | --- |
| Product Code | 158 |
| ISO Viscosity Grade | 320 |
| AGMA Grade | 6 |
| API Gravity | 27.1 |
| Density lb/gal | 7.43 |
| Viscosity @ 40°C, cSt | 360 |
| Viscosity @ 100°C, cSt | 25.5 |
| Viscosity @ 104°F, SUS | 1620 |
| Viscosity @ 212°F, SUS | 122 |
| Viscosity Index | 95 |
| Pour Point, °F, typ. | 20 |
| Flash Point, °F, ASTM D 92 | 400 |
| Copper Corrosion ASTM D 130 | 1a |

Features/Benefits

- Excellent Wear Protection.

- Ready Separation from Condensate.

- Resistant to Deposit Formation at High Temperatures

150 Super Cylinder Oil is recommended for low pressure saturated steam systems.  It may also be used for couplings, bearings, splash-lubricated worm gear sets operating at moderate to high speeds and temperatures and for the break-in of compressor cylinders.

Description

150 Super Cylinder Oil is a blend of high quality base stocks and lubricity additives.  Specifically formulated for Steam Cylinder lubrication, it can also be used for lubrication of slow speed industrial gear applications, worm drives and slow speed loaded journal bearings.

150 Super Cylinder Oil is formulated to withstand higher temperatures with excellent resistance to thermal degradation.  This product protects against rust and corrosion, provides good sealing film strength, excellent lubricity and is resistant to water washout.

150 Super Cylinder Oil

Premium Steam Cylinder Oil

Rev. 2/2024